ILLINOIS TOLLWAY									AC-150

CHECKLIST FOR
HOT- MIX ASPHALT (HMA) PAVEMENT (FULL DEPTH)

This checklist has been prepared to provide the field inspector a summary of easy-to-read, step-by-step requirements relative to the proper construction of Hot-Mix Asphalt Pavement (Full Depth).  The following questions are based on and referenced to information found in the Tollway supplemental Specifications, Tollway Standards, IDOT Standard Specifications, IDOT Highway Standards, IDOT Construction Manual, and current policy memorandums and letters.

Have you checked the contract Special Provisions, Supplemental Specifications and plans to see if any modifications have been made to the requirements listed herein?	____

# 1.	GENERAL

Is the HMA Pavement (Full-Depth) being constructed according to the applicable portions of Section 406 of the Standard Specifications?  Review the applicable requirements in the Construction Inspector’s Checklist for HMA Binder and Surface Course.	____

# SUBGRADE

Is the subgrade prepared according to Section 301 of the Standard Specifications except Articles 301.05 and 301.06 will not apply?  (Art. 407.05)	____

If a lime modified soil layer is specified, is it constructed in accordance with Section 302 of the Standard Specifications?	____

a.	The lime-modified soil layer shall be compacted to not less than 95% of the standard dry density.  The in place density of the completed subgrade will be tested at least every 1500 ft.	____

b.	The surface of the lime-modified soil shall be brought to true shape and correct elevation according to Article 301.07.	____

c.	Trimmings from the lime treated subgrade shall be removed prior to placement of the binder course.  (Art. 407.06)	____

# PLACEMENT

Is the HMA binder and surface courses placed according to Article 406.06 and the following?

The compacted thickness of the initial lift of binder course shall be 4 inches 
thick.	____

Succeeding binder lifts shall be the minimums specified in Article 406.06(d) but no more than 4 inches thick when compacted.	____

The compacted lift thickness of the layers of binder excluding the top lift may be increased to 6 inches if a vibratory roller is used for breakdown, and the required density is obtained.	____

Longitudinal joints shall be constructed in accordance with Article 406.06(g).	____

Each lift of compacted HMA mixture shall be clean when the next lift is placed.	____

A light fog of prime coat shall be applied between lifts of HMA, when directed by the Engineer.	____

a.	The application rate shall be 0.02 gal./square yard	____

# HAULING ON PARTIALLY COMPLETED PAVEMENT

Are trucks only permitted on partially completed pavement only to deliver bituminous mixture to the paver, except that hauling on partially completed segments will be permitted according to the following table.  (Art. 407.08)	____

| Load Limit Restrictions |  |  |
| --- | --- | --- |
|  | Type of Hauling Traffic |  |
| Total Lift Thickness in | Below 85OF | 85oF & above |
| 4-7 inches* | Unloaded | None |
| 7-9.5 inches* | Legally Loaded | Unloaded |
| Greater than 9.5 inches** | Legally Loaded | Legally Loaded |

٭  With the last lift having cooled a minimum of 24 hours.

٭٭  With the last lift having cooled a minimum of 12 hours.

A traffic pattern shall be established that prevents “tracking” of vehicles one directly behind the other.	____

Crossovers shall be used to transfer haul trucks between roadways.	____

a.	Spaced not less than 1000 ft apart.	____

b.	Constructed of a material that prevents tracking dust or mud on the completed HMA layers.	____

c.	Constructed, maintained and removed at the contractor’s expense.	____

# PIPE UNDERDRAINS

Placement of underdrains, when specified, should be in accordance with Section 601 of the Standard Specifications and Standard 601001.	____

Construction of underdrains shall not be started until at least 9.5 in of bituminous concrete binder is placed.  (Art. 407.07)	____

Material excavated from the underdrain trench shall not be deposited or windrowed on any portion of the full-depth pavement.  (Art. 407.07)	____

# SURFACE TESTS

The finished surface of the pavement shall be tested using a California Profilograph or a 16 ft straightedge.  (Art. 407.09)

16 ft straightedge will be used on the following pavement surfaces:

- Locations listed in the following Table shall be tested in the wheel path with the 16 ft straightedge set to the tolerance specified.	____

| Location | Tolerance |
| --- | --- |
| Ramps, Loops and Climbing Lanes | 1/4 in |
| Mainline Gaps ≤ 0.1 mile | 1/4 in |
| Bridge Approaches | 1/4 in |
| Side Roads & Side Streets > 600 ft in length | 1/4 in |
| 50 ft from Bridge Approaches, Wideflange Beam Terminal Joint, Existing Pavement or Mainline Gaps | 1/4 in |
| All curves ≤ 1000 ft radius including SE transitions | 3/8 in |
| Acceleration Deceleration Lanes | 3/8 in |
| Side Streets ≤ 600 ft in length | 3/8 in |
| Turn Lanes, Storage Lanes and Crossovers, Etc. | 3/8 in |
| Intersections | 3/8 in |

b.	Mainline pavements with less than or equal to 40 mph will be tested in the wheel paths with a 16 ft straightedge set to a 
3/16 in tolerance.	____

c.	Mainline pavements with greater than 40 mph with a net project length of less than 1 mile will be tested in the wheel path with a 16 ft straightedge set to a 3/16 in tolerance.	____

d.	All surface variations that exceed the above tolerance shall be removed with an approved grinding device consisting of multiple saws.	____

e.	You the Contractor will furnish and provide jobsite transportation for the 16 ft straightedge.	____

Profilograph – All mainline pavement shall be tested with a California Profilograph, except the mainline pavement previously specified for testing with a16 ft straightedge.	____

a.	The Profile Index and Price Adjustments will be determined in accordance with Article 407.09(b)(1).	____

b.	Corrective work will be in accordance with Article 407.09(b)(2).	____

# THICKNESS TESTS

Is the determination of the pavement thickness performed in accordance with Article 407.10?	____