ILLINOIS TOLLWAY									AC-170

CHECKLIST FOR
CONTINUOUSLY REINFORCED PCC PAVEMENT

This checklist has been prepared to provide the field inspector a summary of easy-to-read step-by-step requirements relative to the proper construction of Continuously Reinforced PCC Pavement (Section 421).  The following questions are based on information found in the IDOT Standard and Supplemental Specifications, IDOT Highway Standards, IDOT Construction Manual and current policy memorandums and letters and Tollway Supplemental Specifications.

Have you checked the contract Special Provisions, Supplemental Specifications and plans to see if any modifications have been made to the requirements listed herein?	____

# DRAINAGE

Is the subgrade being kept drained during all operations?  Are all berms of earth deposited adjacent to the grade being kept drained by cutting lateral ditches through the berms? (Article 301.09)	____

2.	SUBGRADE AGGREGATE

Has the Subgrade Aggregate Source been approved? 		____

If existing Concrete is to be recycled as the PGE component of the Subgrade Aggregate, does it meet the following requirements:

- Has the concrete removal method been approved by the CM?		____

- Are the bituminous and concrete materials being removed and separated as specified without contamination of dirt and foreign matter?		____

- Are stockpiling pads being provided at the crushing location?		____

- Do the PGE aggregate gradations comply with the specifications for the proposed material source?		____

- Does the PGE aggregate contain steel slag or any material that is considered expansive by the Tollway? 		____

Is the PGE component of the Subgrade Aggregate being placed and compacted uniform in gradation?		____

If reclaimed asphalt pavement (RAP) of the shoulders or overlays is to be recycled as the capping stone component of the subgrade aggregate, does it meet the following requirements:

- Is 100% of the processed RAP passing the 3 inch (75 mm) sieve?		____

- Is the processed RAP well graded down through the fines?		____

- Do all portions of the RAP capping stone contain less than 10% steel slag?		____

Has each lift of the Subgrade Aggregate been compacted to obtain the desired keying or interlock and necessary compaction?		____

# 3.	SUBGRADE/SUBBASE TRIMMING

Has the subgrade or subbase been trimmed prior to paving? (Article 420.04)	____

Is the trimming being done with a subgrade machine that meets the requirements of Article 1103.09 prior to paving? (Article 420.04)	____

# 4.	SUBBASE THICKNESS TEST

After trimming, is the thickness of the subbase being checked by any method at every 250 ft location or less?	____

Are all these job control thickness tests being recorded and retained as part of the job records? (Articles 311.07 or 312.31)	____

If locations of subbase have a deficient thickness, are they being corrected according to Articles 311.07 or 312.31 for the type of construction involved?	____

# 5.	PAVING FORMS

If paving forms are used do they meet the following requirements:

Are the forms:  metal, not less than 10 ft in length, equipped with both pin locks and joint locks? (Article 1103.05)	____

Are the forms straight according to the following? (Article 1103.05)	____

a.	The form shall not deviate more than 1/16 inch from a straight
line along the length of its upper edge.

b.	The longitudinal axis of the upstanding leg of the form shall not deviate from a straight line more than ¼ inch in 10 ft of length along the length of its front face.

Is the height of form face not less than edge thickness of proposed pavement, the base width equal to or greater than the height, and are 3 steel pins being used to secure each section? (Articles 1103.05 & 420.06)	____

Are the forms being set on a hard and true grade, built up in ½ inch maximum lifts of granular material in low areas (without using wooden shims) set not less than required for at least one days paving in front of the paver, and cleaned and oiled prior to the placing of concrete? (Article 420.06)	____

When wooden forms are allowed, are they full depth, smooth, free of warp, not less than 2 in thick when used on tangent, and securely fastened to line and grade? (Article 1103.05)	____

Are curved forms of metal or wood being used on curves of 100 ft radius or less? (Article 1103.05)	____

Note:	Forms shall stay in place a minimum of 12 hours after concrete placement.

# 6.	FORM ALIGNMENT

Are you the Contractor checking the forms for line and grade and making necessary adjustments prior to concrete placement? (Article 420.06)	____

# 7.	WIDE FLANGE BEAM JOINT

If wide flange beam joint anchorages are specified, are they staked and checked for dimensions and rebar placement as shown in the plans?	____

# 8.	SUPERELEVATION STAKING

Are you examining the plan curve data for all curves to determine where to stake the beginning and ending stations for all superelevation transitions?	____

By knowing these points and intermediate points, a smooth transition from crown to super can be constructed.

# 9.	PLANT & MATERIALS APPROVAL

Has the plant where the concrete is to be produced been approved?
(Article 1103.02)	____

Have you the Contractor notified the Engineer of his/her proposed sources of materials prior to delivery?  (Article 106.05 of the Tollway Supplemental Specifications)	____

Has all material been inspected, tested and approved before incorporation in the work?  (Article 106.04 of the Tollway Supplemental Specifications)	____

Is this project set up as Quality Control/Quality Assurance (QC/QA)?	____

If so, are you reviewing the latest version of the QC/QA documents for information regarding quality control procedures by the contractor and quality assurance by the Tollway?	____

Note:	Most PCC paving projects will be QC/QA.  The QC/QA requirements will apply to both the PCC pavement and the stabilized subbase if it is constructed of CAM II.

# 10.	TEMPERATURE LIMITATIONS (Article 1020.14(a))

Is the outside air temp in the shade at least 35 °F  and ascending before allowing you the Contractor to start mixing and placement operations?	____

Are you discontinuing your operations when a descending air temp reaches 40 °F?	____

Is the temp of the concrete between 50 °F and 90 °F at the time of placement?	____

# 11.	REINFORCEMENT

Is the reinforcement being supported on the prepared subbase by steel chairs fabricated with sand plates? (Article 421.04(a))	____

Are the transverse tie bars supported in an approved assembly or tied to the underside of the longitudinal reinforcement? (Article 421.04(6))	____

Are the locations and lengths of lap for bar or fabric reinforcement in conformance with the details shown in Tollway Standard A12?	____

Are all bar and fabric laps being tied? (Article 421.04(a))	____

# 12.	MIXING CONCRETE (Article 1020.11)

Are you the Contractor producing the concrete in conformance with one of the following methods?  Check each article for a review of requirements and restrictions for each:	____

a.	Stationary mixer. (Articles 1103.01(a) & 1020.11(a)(2))	____

b.	Transit mixed concrete. (Articles 1103.01(b) &1020.11 (a)(2))	____

# 13.	TRUCK REQUIREMENTS

Is all concrete which is mixed in a stationary mixer being deposited within 30 minutes from the time stamped on the ticket when hauled in nonagitating trucks and within 60 minutes when hauled in mixing or agitor trucks? (Article 1020.11(a)(7))	____

Is truck mixed concrete being delivered and deposited within 60 minutes from the time stamped on the ticket? (Article 1020.11(a)(7))	____

Note:	Haul time may be increased to 90 minutes if the air temperature is between 50˚F and 64˚F or if a retarder is used.	____

Are you the Contractor planning to use previously placed pavement as a haul road, are you checking trucking weights to assure compliance with maximum weights as permitted by the Tollway? (Articles107.04 & 107.16 of the Tollway Supplemental Specifications.)	____

# 14.	SEQUENCES OF FORM TYPE PAVING

Is all of the required concrete finishing equipment on the job and in acceptable working condition?  Are the following sequences for form type paving being properly followed:

a.	Placing concrete (Article 420.07).  Is the concrete being unloaded into a mechanical concrete spreader?  (Article 1103.12)	____

Note:  Use of a mechanical concrete spreader may be waived if the
concrete hauling equipment is equipped with a discharge system capable of distributing the concrete without segregation. (Article 1103.13)

b.	Strike-off (Article 420.09).  Is the concrete being struck off to the cross section of the proposed pavement?	____

c.	Consolidation (Article 420.09).  Is one pass of an approved surface vibrator (minimum of 3500 VPM) or internal vibrator (minimum of 7000 VPM) (Article 1103.12) being made?  Are you checking the vibrator frequency at the start of each day with a reed tachometer?	____

d.         Finishing (Article 420.09(a))

(1)	Is the concrete being finished by an approved finishing machine?  (Article 1103.13(b))	____

or;

(2)	When breakdowns occur, hand methods will be permitted to finish up deposited concrete. (Article 420.09(a)(2))	____

or;

(3)	When pavement width varies or is less than 10 ft in width, vibrating screed may be used for strike-off and consolidation. (Article 420.09(a)(3))	____

e.	Longitudinal floating (420.09(b))

(1)	Is the form riding mechanical float (Article 1103.15) making 2 passes over all areas? (Article 420.09(b)(1))	____

or;

(2)	Form riding finisher float (Article 1103.14) suspended on rigid frame? (Article 420.09(b)(2))	____

or;

(3)	(In emergency or for pavements with a speed limit posted at 40 m.p.h. or less), 12 ft x 6 inches hand operated longitudinal float (Article 1103.17(e)). (Article 420.09(b)(3))	____

f.	Straightedging (Article 420.09(c)) - At least two 10 ft long straight edges shall be supplied. (Article 1103.17(h))	____

g.	Edging (Article 420.09(d)) - At least two 1/4 inch radius edging tools. (Article 1103.17(j))	____

h.	Final Finish (Article 420.09(e)) – For a type A finish, is the surface of the concrete textured with a turf drag followed by a mechanically operated metal comb transverse grooving device (tining)?	____

A type B finish only requires a turf drag.

i.	Do you the Contractor have available at all times a covering material such as polyethylene sheeting for the protection of the pavement in case of rain? (Article 420.07)	____

# 15.	SEQUENCES OF SLIPFORM PAVING

When you use this optional method for the construction of the pavement are the following sequences being properly followed:

a.	Is the self propelled formless paver (Article 1103.16) capable of spreading, striking off, consolidating internally and finishing the newly placed concrete in one pass to the required line and grade?
(Article 420.14)	____

b.	Are you checking the vibrator frequency at the start of each day with a contractor furnished reed tachometer? (Article 1103.12)	____

c.	Is the pavement being floated, straightedged, edged and textured as described in Item 14?  (Article 420.09)	____

d.	Do you the Contractor have available at all times metal or wooden sideforms and a covering material such as polyethylene sheeting for the protection of the pavement in case of rain? (Article 420.07)	____

e.	Are you the Contractor immediately repairing all slumping edges in excess of 1/2 inch or ¼ inch if additional concrete work is required adjacent to the pavement lane being placed? (Article 420.14(c))	____

# 16.	THICKNESS TEST

Are you checking the thickness of the pavement at least at every 250 ft 
location? (Before and after rod and level, before and after stringline, or direct probing measurements are all acceptable.)  Record and retain in job records.  (Articles 420.15 & 407.10)	____

# 17.	AIR CONTENT

Are you testing the concrete for air (5 - 8%) at least every 250 ft of pavement? Record and retain in job records. (Articles 1020.08 & 1020.04 Table 1)	____

# 18.	SLUMP

Are you testing the concrete for slump (2 to 4 inches, or ¾ to 
1½ inch when slipforming) at least once each day?  Record and retain in job records. (Articles 1020.07 & 1020.04 Table 1)	____

# 19.	REINFORCEMENT DEPTH CHECKS

Are you periodically probing the concrete to check the vertical positioning of the pavement reinforcement?  Article 421.04(a) for tolerances.  Record and retain in job records.	____

# 20.	STRENGTH

Are test specimens being cast at the site of work at the following frequency:	____

a.	Modulus of Rupture 6” x 6” x 30” beam (Standard Method of Test for Making and Curing Concrete Test Specimens in the Field and Appendix C):

4 beams first day; 2 per day thereafter.

Break @ 3, 5, 7 and 14 days.

Strength requirement = 650 psi in 14 days
(Article 701.17(c)(5))

Report on Form MI 655, “Field Record Book of Modulus of Rupture Tests of Concrete Beams”	____

or;

b.	Compressive Strength 6” dia. x 12” cylinder. (Standard Method of Test for Making and Curing Concrete Test Specimens in the Field and Appendix C)

Make 2 cylinders in lieu of each beam (Sampling Schedule 3 of the EQP Specifications or Special Provisions)

Strength requirement = 3500 psi in 14 days
(Article 701.17(c)(5))

Note:   	For QC/QA projects, see sampling frequency for the contractor’s quality control and the Tollway’s quality assurance in the Recurring Special Provision.

# 21.	Sawed LONGITUDINAL JOINT (Std. 420001 & Article 421.04(b)(1))

a.	Is the longitudinal joint strengthened by 30 inch - #6 tie bars at 30 inch centers at t/2 depth perpendicular to the joint? (Article 420.05(a))	____

b.	Sawing of the longitudinal joint may commence as soon as the concrete has hardened sufficiently to permit sawing without excessive raveling.  The saw cut shall be made to a depth of t/3 of the pavement thickness. (Article 420.05(a))	____

# 22.	TRANSVERSE EXPANSION JOINTS

a.	Is the preformed joint filler continuous from form to form, shaped to the subbase (or subgrade)? (Article 420.05(d))	____

b.	Are the smooth dowel bars positioned parallel to the grade @ t/2 depth and @ 12 inch centers? 	____

c.	Are the capped ends of the bar oiled? (Article 420.05(d)(2))	____

# 23.	TRANSVERSE CONSTRUCTION JOINTS (Article 421.04(b))

a.	Are transverse construction joints placed at the end of each day’s operation or after an interruption in the concreting operation of 30 minutes or more?	____

b.	Are joints at least 3 ½ feet from nearest bar lap?	____

c.	Are joints strengthened by supplementary 6 foot long No. 6 (No. 20) bars placed between normal longitudinal steel? 	____

d.	Are the transverse construction joints formed by means of a clean (not oiled) split header board conforming to the cross section of pavement?	____

e.	Is the concrete internally vibrated along the length of the joint and the area that extends 10 ft from the joint, both at the end of the current operation and once again in the new concrete at the resumption of placement?

# 24.	SURPLUS - DEFICIENCY DETERMINATION

Is a daily check being made on the yield of produced concrete?  A deficiency computation is serious; it usually indicates thin pavement.	____

D or S = Required Volume − Volume UsedRequired Volume x 100

Where - Required Volume = L’ x W’ x D’ x 1/27

Used Volume = Number of batches x cy /batch

# 25.	CURING

Are the pavement surface and edges being cured for 3 days 
(Article 1020.13(a)) by one of the following methods:

a.	Waterproof Paper Method. (Article 1020.13(a)(1))	____

b.	Polyethylene Sheeting Method. (Article 1020.13(a)(2))	____

c.	Wetted Burlap Method. (Article 1020.13(a)(3))	____

d.	Membrane Curing Method.  As soon as water sheen has disappeared, are 2 separate applications, separated by at least one minute, of agitated Type III (white) curing compound (1022.01) being uniformly applied at a rate of one gallon/250 sf? 
(Article 1020.13(a)(4))	____

Note:  Not allowed between November 1 & April 15 
	(Article 1020.13 Note 5).  Not allowed if protective coat is to be 	applied. (Article 1020.13(a)(4))

e.	Wetted Cotton Mat Method. (Article 1020.13(a)(5)

# 26.	PROTECTION

Are you the Contractor providing protection of the pavement from low temperatures as follows: (Article 1020.13(c))

Min. Temp. Forecast 		Protection

25°F - 32° F	1 layer of poly & 1 layer burlap, or

(or if drops below 32° F	2 layers of polyethylene, or

during first 72 hours)	2 layers of waterproof paper	____

Below 25°F	6 inches of straw

covered with 1 layer of poly or

waterproof paper	____

# 27.	SURFACE VARIATIONS

When the concrete has cured sufficiently to permit the testing, are you profilographing or straight-edging each wheel lane for surface variations? (Articles 420.10 & 407.09)	____

Is the required corrective work being performed? (Articles 420.10 & 407.09)	____

# 28.	OPENING TO TRAFFIC

Is the pavement being closed to traffic until:

a.	The curing and protection period has elapsed?	____

b.	All joints have been sealed? (Article 420.12)	____

Note:  The pavement shall also be closed to construction traffic until
	the joints are sealed.

c.	The required strength has been achieved by test specimen?	____

If you the Contractor wishes to open the pavement to traffic prior to the date of your first routine beam break, are additional specimens being cast and then allowed to cure out in the open the same as the pavement? (Manual of Test Procedures for Materials, Standard Method of Test for Making Curing Concrete Test Specimens in the Field)	____

# 29.	PROTECTIVE COAT

a.	Is a protective surface treatment being applied when pavement is constructed after October 15, and will be opened to traffic prior to the following April 15; or when directed by the CM? (Article 420.18)	____

b.	Are 2 coats at 50 sy/gal coat being applied to 14 day old minimum pavement?  Is air temperature above 40 °F?
(Article 420.18)	____

# 30.	REMOVAL AND REPLACEMENT OF CR PCC PAVEMENT

If for any reason you are required to replace any of the pavement prior to final acceptance, are the construction requirements of Article 442.05(a) being adhered to?	____

# 31.	FIELD RECORDS

Are all tests, measurements, observations and computations required in the foregoing being maintained in a hard back field book?	____